T. K. Gustafson: April 18 2007
And the many contributers
Confined Waves on Structures- Some Accomplishments
        Possibilities and Open Questions
1) Surface wave coupling as an extension of antenna theory
2) Experiments involving coupling to surface waves at 10 microns
3) The first lumped nonlinear infrared mixing experiments
4) Comments on pumping of plasmons through tunneling
5) Negative resistance and oscillations -Evidence of Surface Wave Pumping?

---
NIST (NBS at this time was using
metal point contact diodes for
frequency referencing to an atomic
standard by harmonic mixing
Appl. Phys. Lett. 17, 8 (1971)
Was referrng mostly to H20 and
CO2 Lasers at this point in time
Tungsten on polished nickel

---
Indication of the Scale of the Early Etched Tips Obtained at Berkeley
Electron Microscopy Group ( T. E. Everhart and Jerome Wiesner )

---
The Vertical Configuration
of Early Antenna Coupled
Experiments (Improved
Etching Techniques)
Tungsten touched to Gold Illuminated With
 He-Ne Beam ( Approx 1972 ) (Berkeley)
Note: This is one wire and its image in
the gold ground plane
Faris Gustafson Wiesner JQE QE9 ,737 (1973)

---
Typical Experiments- Rectification

---
Detection of a He-Ne Laser – Argued that it was lumped NLO Rectification
S. M. Faris, T. K. Gustafson, and J. Weisner, Jour. Quant. Electr. QE-9, 737 (1973)
Current=Voltage
Detected Signal
The Argument
Approx 10-16 seconds

---
Theoretical Calculations Based Upon “Simmon's” Theory of
Tunnelling- Key Principles – Turning Points, Image Charge
and Averaged Barrier
The shapes of the detection characteristics were indeed evidence
that rectification was occurring (ref. Ibid )

---
Surface Wave Extensions to Antenna Theory
A-Open Surface
B- Gap Mode
C-Transition Region
Dispersion relation for the open surface mode
D. P. Siu and T. K. Gustafson
Appl. Phys. Lett., 31, 71 (1977)

---
The Gap Mode
Dispersion relation of the gap mode for the
(even function of z)
Ex is an odd function of z
Ex = E0 i u2 / kg tanh ( u 2 d ) sinh( u2 z ) / sinh ( u2 d )
Dispersion relation : u 1 d = u2 d ( - e 1 )/ ( e 2 ) tanh ( u2 d )
It is assumed that the coupling is through Ex which excites open surface modes propagating away (toward) the junction
via the current. (ref. Ibid )

---
The Coupling Model Which Extends Antenna Theory For The “Gap” Mode
For antenna theory current excitation is assumed which is the z-directed
Electric Field Component.
e1
e2
( Metal )
(e2 )
Gap
Note: Ex has a discontinuous
sgn jump at the junction in the
limit as the gap width goes to
zero. Hy and Ez are continuous.
Ez assumed to be zero at
Z= L and -L ( antenna length
is 2 L )
Region A
( ref. Ibid )

---
Approximate Field Pattern in Region A
( is a single surface plasma standing wave along the antenna)
Assuming zero
Current at z=L
Once the fields are
known along the wire
vector diffraction theory
can be used to calculate
the far fields. (Stratton and
Chu Phys Rev ,56 (1939)
The finite length allows for coupling to the free-space modes
Approximate angle given by Dk L = p
Peak Angle approximately [ ( kfree-space / kplasma )2 – 1 ] + 2 D k / kplasma

---
Calculated Pattern Showing The Influence of Slowing and Loss
2 eV is in the relaxation region of Al.
Al and W
D.P. Siu and T. K. Gustafson

---
Theoretically Calculated Voltage Induced By a Plane Wave
Ref. ibid

---
The Coupling Model For The “Dark Mode” ( Quadrupole Radiator
as suggested by Alexandar Usksov )
For antenna theory current excitation is assumed which is the z-directed
Electric Field Component on the open surface .
e1
e2
( Metal )
(e2 )
Gap
Hy and E z have discontinuous
sgn jumps at Z=0 in the limit of
a small gap on the vertical open
surface.
(Using the vector potential
calculate the radiation pattern
for a finite length 2L in the
Z-direction as a function of
frequency)

---
Experimental Observations at 10 microns (CO2 Laser )
The junction configuration

---
Experimental Results

---
Earlier Work
1993

---
Early Work on Lithographically Fabricated Junctions at “MIT”

---
Twu and Schwarz Analyzed The Detected Signal In terms of Lumped
Antenna Circuit Theory (Point contact diodes at 10 microns )
Appl. Phys. Lett. 28, 596(1974)

---
The Motivation For Broadband Mixing- Frequency Metrology
Taken from
“Application of
Nonlinear Devices
to Optical Frequency
Measurement
D. J. E. Knight and
P.T. Woods, Journal
of Physics E: Scientific
Instruments 1976
Volume 9
If the input frequencies are known and m and n are known then
measuring the I. F. accurately when the output is mixed with
with an L. O. of unknown frequency one accurately determines
the absolute frequency of the L. O.

---
CO2 frequency known by a previous measurement. The klystron frequency
could be measured directly with a frequency counter
 Frequency comb technology produced by self-phase
modulaion of a continuous train of femtosecond pulse in holey
fibers has allowed for the development of frequency markers
(Scott Diddams CLEO-07 Talk JTuC5)

---
A Note on Current Driven Versus Voltage Driven Junctions
5'th Harmonic of a
signal beating with a
local oscillator.
Experimentally detected
signal
(Ref. E. Sakuma and K. Evensen
IEEE J. Quaantum Electron.
QE-10, 599 (1974)

---
Theoretical Claculations
S. M. Faris and T. K. Gustafson
Appl. Phys. Lett. 25, 545 (1974)
Harmonic Mixing can be used as a frequency probe.

---
The Bridges Result- Frequency Mixing at Ten Microns
A lumped Nonlinear Parametric Infrared Mixer (T. K. Gustafson and T. J. Bridges
Appl. Phys. Lett. 25, 56 (1974)
More recent Krieger et al (Max Planck) Phys Rev. B 41, 10229 (1990)

---
More Recent Results on Difference Frequency Mixing
Phys. Rev. B , 41, 10229 (1990)
Up to 9 Thz had been demonstrated

---
Excitation of The Gap Mode through Electron Tunnelling : Negative Resistance
and Resonant Tunnelling Devices
Basic Approach:
#The Gap Mode can be described in terms of a potential
        profile- at least in the quasi-static limit
#Tunnelling Electrons scatter off of the potential giving
        up energy to the mode
# We know it works because of ineleastic scattering from
        atoms in the junction ( Lambe-Jacklevic)
# Question? : Can one obtain enough of an excitation to
        overcome the large losses associated with
        the gap mode

---
Lambe Jaklevic – Phys Rev. Lett. 17, 1139 (1966)
Inelastic Tunnelling

---
Tunneling Junction Configuration
T
strained by the junction
Ex (S2 - S1)
UR
(Ref. D. P. Siu and T. K. Gustafson Appl. Phys. Lett., 32, 500 (1978)

---
The wave functions
The wave-functions in the

---
The Transfer Hamiltonian Matrix Element
Problem! Dominated by the more
highly probable absorption process
because the overlap of the wave functions
is much greater. Possible solution
E. M. Belenov, P. N. Luskinovich, V. I.
Romanenko, A. G.Sobolev and A. V. Uskov
Soviet Journal of Quantum Electronics
17, 1348 (1987)
Other relevant reference: : B. N. Kurdy
and D. G. Hall Phys. Rev. B ,14, 3980 (1986)

---
Negative Resistance, Oscillations, and Picosecond Resposes Have Been Observed
Sequence
shows icreasing
resistance as a
tunnelling tip is
drawn back from
a ground plane.
The emergence
of negative
resistance
is evident in
both of these
examples

---
Direct Evidence of Oscillations Due to Negative Resistance

---
Possibilities For Future Efforts
# Use Uskov's quantized approach with the boson field being
    a travelling or standing wave gap mode and the interaction
    a tnnelling interaction rather than a dipole dipole transfer
# Coupled molecular engineered antennas- preferably with gaps a few l
attice spacingsthat exhibit tunnelling ( 10- 1 nm )
# Excitation of the “Symmetric Gap Mode” through the quadrupole antenna
   characteristics
# Tunnelling I-V such that the second derivative of I w.r.t. V is
    much lgreater than ( I (eV+hf) – 2 I(eV) + I (eV-hf ) )
# Surface Plasmons combined with Surface Emitting Laser
Session CthB CLEO 07 Farban et al. (“ ... low-loss laser nanocavities
with sub – wavelength cavities in all three dimensions are feasible” )